CPVC



Submittal Information

PVC Couplings

|  |
| --- |
| * Standard Size Couplings Fabricated From Seamless

Extruded PVC Duct* Additional Custom Sized Couplings Available Upon Request
* Couplings Are Triple-Pass Welded Using 5/32” PVC Welding Rod

-Depending on Size, Coupling May Have 1-2 Seams* All Dimensions in Inches
* All Dimensions are to CSSI Standards and are Subject

To Change |
|  |
|  |

PRODUCT DIMENSIONS

|  |
| --- |
|  |

 PVC COUPLINGS SUBMITTAL INFORMATION

 Model Number Nominal Duct Size Average Duct O.D. Average Wall Thickness A B

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  CP-PVC-6 | 6 | 6.625 | 0.187 | 6.625 + 1/16 | 4 |
|  CP-PVC-7 | 7 | 7.375 | 0.187 | 7.375 + 1/16 | 4 |
|  CP-PVC-8 | 8 | 8.625 | 0.187 | 8.625 + 1/16 | 4 |
|  CP-PVC-9 | 9 | 9.375 | 0.187 | 9.375 + 1/16 | 4 |
|  CP-PVC-10 | 10 | 10.75 | 0.187 | 10.75 + 1/16 | 4 |
|  CP-PVC-12 | 12 | 12.75 | 0.187 | 12.75 + 1/16 | 4 |
|  CP-PVC-14 | 14 | 14 | 0.187 | 14 + 1/16 | 4 |
|  CP-PVC-16 | 16 | 16 | 0.187 | 16 + 1/16 | 4 |
|  CP-PVC-18 | 18 | 18 | 0.187 | 18 + 1/16 | 4 |
|  CP-PVC-20 | 20 | 20 | 0.219 | 20 + 1/16 | 6 |
|  CP-PVC-24 | 24 | 24 | 0.25 | 24 + 1/16 | 6 |

“B” END TYPE